## Slide 1
AN INTRODUCTION TO NORTH AMERICAN HARDWOODS
Lumber Grades & Species
DANA SPESSERT
Chief Inspector, NHLA

## Slide 2
Education
Promotion
Advocacy
Networking
Industry Services
Main Roles of NHLA

## Slide 3
NHLA RULES
Established more than 100 years ago.
One of the only standard grading systems in the world.

## Slide 4
Measurable Percentage of Clear Wood
Determines Both Cost and Waste Factor
Cuttings (Pieces)
  Size
  Number
Basic Principles of Grading Hardwoods

## Slide 5
Grading from the poor side
Each clear area of the board is measured and considered a “cutting” if large enough
Clear areas of the board are valued using the Cutting Unit Method
Basic Principles of Grading Hardwoods

## Slide 6: Cuttings
Definition of Cutting – Paragraph 29.
A cutting is a portion of a board of plank obtained by cross-cutting or ripping or by both… Diagonal cuttings are not permitted.
Yes
Yes
No
Yes
Yes
Yes

## Slide 7
MEASUREMENT
CONVERSION FACTORS
1” = 4/4 = 25.4mm
2” = 8/4 = 50.8mm
1m= 3.281ft
*Average lengths are 7-12ft
1000bf (1MBF) = 2.36m3
12,000bf = 28.3m3
1m3 = 424 board feet (BF)
1m3 = 35.315 cubic feet(cu.ft)

## Slide 8: Cutting Unit Method
The percentage of cutting in a board is determined under the
Cutting Unit Method. Cutting unit is 1 inch by 1 foot:
1”
12”
12”
One square foot
contains 12 cutting units:
12”

## Slide 9
SURFACE MEASURE & BOARD FEET
SM = multiply the width of the board in inches by the length of the board in feet and divide the sum by 12, rounding up or down to the nearest whole number.

## Slide 10
GRADING SCALE

## Slide 11
EXAMPLE OF FAS (RED OAK)

## Slide 12
FAS REQUIREMENTS

## Slide 13
Wane
12’
6”
Knot
SM = 6” x
12’ ÷ 12 = 6’
Number of Cuttings for FAS:
SM ÷ 4 = 6/4 = 1½ = 1 cutting
Cutting Units needed for FAS: SM x 10 = 6 x 10 = 60 C.U.
  6” x 10’ = 60 C.U.

## Slide 14
Wane
12’
12”
Knot
SM = 12” x 12’ ÷ 12 = 12’
Number of Cuttings for FAS: SM
÷ 4 = 12/4 = 3 cuttings
Cutting Units needed for FAS: SM x 10 = 12 x 10 = 120 C.U.
42 + 39 + 40 = 121 C.U.
6” x 7’ = 42 C.U.
8” x 5’ = 40 C.U.
6” x 6½’ = 39 C.U.

## Slide 15
Knot
Wane
12’
8”
SM = 8” x 12’ ÷ 12 = 8’
Number of Cuttings for FAS:
SM ÷ 4 = 8/4
= 2 cuttings
Cutting Units needed for FAS: SM x 10 = 8 x 10 = 80 C.U.
24 + 60 = 84 C.U.
3” x 8’ = 24 C.U.
5” x 12’ = 60 C.U.

## Slide 16
FAS APPLICATIONS

## Slide 17
FAS APPLICATIONS

## Slide 18
FAS APPLICATIONS

## Slide 19
EXAMPLE OF No 1 COMMON (RED OAK)

## Slide 20
No 1 COMMON REQUIREMENTS

## Slide 21
No 1 COMMON REQUIREMENTS
If better face meets FAS and poor face makes No 1 Common the grade has potential to be F1F or selects.

## Slide 22
Wane
8’
6”
Wane
SM
= 6” x 8’ ÷ 12 = 4’
Number of Cuttings for #1 Com:
SM+1 ÷ 3 = 5 ÷ 3
= 1 cutting
Cutting Units needed for #1 Com: SM x 8 = 4 x 8 = 32 C.U.
4” x 8’ = 32 C.U.
#1 Common

## Slide 23
Knot
Wane
12’
12”
Wane
SM = 12”
x 12’ ÷ 12 = 12’
Number of Cuttings for #1Com: SM+1 ÷ 3 = 13 ÷ 3 = 4 cuttings
Cutting Units needed for #1Com: SM x 8 = 12 x 8 = 96 C.U.
15¾ + 20¼ + 38¼ + 34 = 108¼ C.U.
3½” x 4½‘ = 15¾ C.U.
4½” x 4½’ = 20¼ C.U.
8½” x 4½’ = 38¼ C.U.
6” x 5 2/3’ = 34 C.U.
#1 Common

## Slide 24
Knot
Wane
12’
7”
Wane
SM = 7” x 12’ ÷ 12 = 7’
Number of Cuttings for #1 Com:
SM+1 ÷ 3 = 8÷3
= 2 Cuttings
= 56.
Cutting Units needed for #1 Com: SM x 8 = 7 x 8
24 + 44 = 68 C.U.
3” x 8’ = 24 C.U.
4” x 11’ = 44 C.U.
#1 Common

## Slide 25
No 1 COMMON APPLICATIONS

## Slide 26
EXAMPLE OF No 2 COMMON (RED OAK)

## Slide 27
No 2 COMMON REQUIREMENTS
2A Common is clear cuttings
2B Common is sound

## Slide 28
No 2 COMMON REQUIREMENTS

## Slide 29
Wane
Knot
9’
7”
Wane
SM = 7” x 9’ ÷
12 = 5’
Number of Cuttings for #2A Com:
SM ÷ 2 = 2 cuttings
Cutting Units needed for #2A Com: SM x 6 = 5 x 6 = 30
20 + 15 = 35 C.U.
Clear-face cuttings
C.U.
6” x 2½’ = 15 C.U.
#2A Common
4” x 5’ = 20 C.U.

## Slide 30
Wane
Wane
12’
12”
Knot
Knot
SM = 12” x 12’ ÷ 12
Number of Cuttings
= 12’
for #2 Com:
SM ÷ 2 = 12÷2 = 6 Cuttings
Cutting Units needed for #2 Com: SM x 6 = 12 x 6 = 72 C.U.
10 + 18 + 14 + 42 = 84 C.U.
Clear-face cuttings
12” x 3½’ = 42 C.U.
3½” x 4’ = 14 C.U.
#2A Common
6” x 3’ = 18 C.U.
5” x 2’ = 10
C.U.

## Slide 31
Wane
Checks
Wane
12’
12”
Worm holes
Knot Split
SM = 12” x 12’ ÷ 12
Number of Cuttings
= 12’
for #2 Com:
SM ÷ 2 =
12÷2 = 6 Cuttings
Cutting Units needed for #2 Com: SM x 6 = 12 x 6 = 72 C.U.
10 + 18 + 14 + 42 = 84 C.U.
Sound cuttings
12” x 3½’ = 42 C.U.
6” x 3’ = 18 C.U.
5” x 2’ = 10
C.U.
3½” x 4’ = 14 C.U.
#2B Common

## Slide 32
No 2 COMMON APPLICATIONS

## Slide 33
Characteristics Allowed in Clear Face Cuttings

## Slide 34
Characteristics Allowed in Clear Face Cuttings

## Slide 35
Characteristics Not Allowed in Clear Face Cuttings

## Slide 36
Characteristics Not Allowed in Clear Face Cuttings

## Slide 37
Characteristics Not Allowed in Clear Face Cuttings

## Slide 38
NHLA
Grading
Chart
Common
1½”wide
square inches
sound
FAS
F1F
Select
#1 Common
#2A & #2B Common
#3 A Common
#3 B
Minimum
Board Size
6’’ x 8’
6’’ x 8’
4’’ x 6’
3’’ x 4’
3’’ x 4’
3’’ x 4’
3’’ x 4’
Minimum
Cutting Size
4’’x 5’
3’’x 7’
Better Face to
Grade FAS
Poor Face to
Grade #1
Common
4’’x 2’
3’’x 3’
3’’ x 2’
3’’ x 2’
Not less than
containing 36
Basic Yield
83% or
SM x 10
66% or
SM x 8
50% or
SM x 6
33% or
SM x 4
25% or
SM x 3
Formula to Determine Number of Cuttings
SM
4
(4 max.)
SM+1
3
(5 max.)
SM
2
(7 max.)
Unlimited
Unlimited
cuttings

## Slide 39
KILN DRYING HARDWOOD LUMBER

## Slide 40
ASH SAMPLES

## Slide 41
CHERRY SAMPLES

## Slide 42
HARD MAPLE SAMPLES

## Slide 43
RED OAK SAMPLES

## Slide 44
WHITE OAK SAMPLES

## Slide 45
TULIPWOOD SAMPLES

## Slide 46
WALNUT SAMPLES

## Slide 47
SUMMARY OF US HARDWOOD LUMBER SPECIES

## Slide 48
KEY POINTS WHEN BUYING OR SPECIFYING US HARDWOODS
Know the product
Understand the grades
Communicate with your supplier

## Slide 49
Questions?

## Slide 50
AMERICAN RED ALDER

## Slide 51
AMERICAN RED ALDER

## Slide 52
AMERICAN RED ALDER

## Slide 53
AMERICAN RED ALDER

## Slide 54
AMERICAN RED ALDER

## Slide 55
AMERICAN ASH

## Slide 56
AMERICAN ASH

## Slide 57
AMERICAN ASH

## Slide 58
AMERICAN CHERRY

## Slide 59
AMERICAN CHERRY

## Slide 60
AMERICAN CHERRY

## Slide 61
AMERICAN CHERRY

## Slide 62
AMERICAN HICKORY & PECAN

## Slide 63
AMERICAN HICKORY

## Slide 64
AMERICAN HICKORY

## Slide 65
AMERICAN PECAN

## Slide 66
AMERICAN HARD MAPLE

## Slide 67
AMERICAN HARD MAPLE

## Slide 68
AMERICAN HARD MAPLE

## Slide 69
AMERICAN SOFT MAPLE

## Slide 70
AMERICAN SOFT MAPLE

## Slide 71
AMERICAN RED OAK

## Slide 72
AMERICAN RED OAK

## Slide 73
AMERICAN RED OAK

## Slide 74
AMERICAN RED OAK

## Slide 75
AMERICAN WHITE OAK

## Slide 76
AMERICAN WHITE OAK

## Slide 77
AMERICAN WHITE OAK

## Slide 78
AMERICAN WHITE OAK

## Slide 79
AMERICAN TULIPWOOD (YELLOW POPLAR)

## Slide 80
AMERICAN TULIPWOOD (YELLOW POPLAR)

## Slide 81
AMERICAN TULIPWOOD (YELLOW POPLAR)

## Slide 82
AMERICAN TULIPWOOD (YELLOW POPLAR)

## Slide 83
AMERICAN WALNUT

## Slide 84
AMERICAN WALNUT

## Slide 85
AMERICAN WALNUT

## Slide 86
AMERICAN WALNUT